PermaStrip:  SHORT SPECIFICATION

Place the following in specification section that will be used for the main landscaping work (for example, Section 32 94 13 Landscaping, or etc.).  The architect to edit size, thickness, length, and finish required for the project.  Comments shown in “italics.”

PART 1 	GENERAL

1.01	WARRANTY

Actual article number will be determined by location within the Part 1 portion of specification.

A.	15-year limited material warranty for landscape edging from manufacturing defects in workmanship or material.

PART 2 	PRODUCTS

2.01	PLANTING ACCESSORIES

Actual article number will be determined by location within the Part 2 portion of specification.

A.	Heavy Duty L-Shaped Profile Maintenance Strip Edging:  Permaloc PermaStrip, 1/8 inch (3.2 mm) x 3-1/2 inches (89 mm) high, 3/16 inch (4.8 mm) x 3-1/2 inches (89 mm) high, 1/8 inch (3.2 mm) x 4 inches (101.6 mm) high, 3/16 inch (4.8 mm) x 4 inches (101.6 mm) high, 1/8 inch (3.2 mm) x 6 inches (152.4 mm) high, 3/16 inch (4.8 mm) x 6 inches (152.4 mm) high extruded aluminum, 6063 alloy, T-6 hardness, maintenance strip edging for straight-line and gentle curve applications in corrugated L-shaped profile having 1.2 inch (30.5 mm) horizontal base, as manufactured by Permaloc Corporation, Holland MI 49424, telephone (800) 356-9660 or (616) 399-9600.  Section shall have loops on side of section to receive stakes spaced approximately 2 feet (610 mm) apart along its length.

B.	Thickness:  1/8 inch (3.2 mm) gage section at 0.060 inch (1.52 mm) minimum thick with 0.200 inch (5.1 mm) exposed top lip and 3/16 inch (4.8 mm) gage section at 0.076 inch 1.93 mm) minimum thick with 0.190 inch (4.8 mm) exposed top lip.

C.	Length:  8 and 16 feet (2.44 and 4.88 meters).

D.	Connection Method:  Section ends shall splice together with a horizontal 0.060 inch (1.52 mm) thick x 1 inch (25 mm) wide x 4 inches (102 mm) long aluminum sliding connector.

E.	Stake:  12 inch (305 mm) Permaloc Standard Stake, 0.10 inch (2.5 mm) thick, with optional extruded aluminum, heavy duty 0.125 inch (3.2 mm) thick x 16 inches (406 mm), 18 inches (457 mm), or 24 inches (610 mm) long stakes.  Stakes to interlock into section loops.

F.	Finish:  Natural Mill Aluminum and Black DuraFlex Painted.  Paint finish shall comply with AAMA 2603 for electrostatically baked on paint.

PART 3 	EXECUTION

3.01	LANDSCAPE EDGING INSTALLATION

Actual article number will be determined by location within the Part 3 portion of specification.

A.	Preparation:  Ensure that all underground utility lines are located and will not interfere with the  proposed edging installation before beginning work.  Locate border line of edging with string or other means to assure border straightness and curves as designed.

B.	Set edging into trench with the horizontal base resting on compacted subbase and top at ½ inch (12.7 mm) above compacted finish grade on turf side.  Loops for stakes are to be placed on the turf side.  Drive stakes through edging loops until locked in place.  Requires 8 stakes evenly spaced for each 16 feet (4.88 meters) section, or 3 stakes evenly spaced for each 8 feet (2.44 meters) section.  Provide longer stakes, heavier gage stakes, or any combination of previously mentioned as necessary to firmly secure edging for permanent intended use.

C.	Where edging sections turn at corners and at angled runs, cut edging partially up through its height from bottom and turn back to desired angle to form rounded exposed radius.

D.	Backfilling and Cleanup:  Backfill both sides of edging, confirm and adjust if necessary that sections are securely held together, and compact backfill material along edging to provide top of edging at 1/2 inch (12.7 mm) above turf finish grade.  Cleanup and remove excess material from site.

August 27, 2014