Permaloc BrickBlock:  SHORT SPECIFICATION

Place the following in specification section that will be used for the main paver work (for example, Section 02780 Paver, or etc.).  The architect to edit size, thickness, length, and finish required for the project.  Comments shown in “italics.”

- GENERAL

  - WARRANTY

Actual article number will be determined by location within the Part 1 portion of specification.

    - 15-year limited material warranty for paver restraint edging from manufacturing defects in workmanship or material.

- PRODUCTS

  - PAVER RESTRAINT EDGING

Actual article number will be determined by location within the Part 2 portion of specification.

    - Product:  PermaLoc BrickBlock, .065 inch (1.65 mm) [.075 inch (1.9 mm)] thick x 1-3/4 inches (44.5 mm) high, extruded aluminum, 6063 alloy, paver restraint edging for straight-line and curvilinear applications in corrugated L-shaped profile, as manufactured by PermaLoc Corporation, Holland MI 49424, telephone (800) 356-9660 or (616) 399-9600.  Horizontal base shall have holes spaced 4 inches (102 mm) apart along its length to receive spikes.

    - Thickness:  .065 inch (1.65 mm) gage section shall have 0.070 inch (1.78 mm) thick exposed top lip, .075 inch (1.9 mm) gage section shall have 0.080 inch (2.03 mm) thick exposed top lip.

    - Length:  8 feet (2.44 meters).

    - Connection Method:  Section ends shall connect together over the top edge with 0.030 inch (.76 mm) thick x 1.25 inch (31.8 mm) wide x .75 inches (19 mm) tall steel clip.

    - Spikes:  3/8 inch x 10 inches (9.5 mm x 254 mm) bright spiral steel spike. Use plastic washers if desired.

    - Finish:

      - Natural Mill Aluminum.

      - Black DuraFlex Painted:  Electrostatically baked on acrylic paint, AAMA 2603, color #PPG UC88182.

- EXECUTION

Editorial Comment (shown in italic):  The following information for base preparation and installation shall be specified in specification section for Paver and is recommended only as a generally accepted paver installation method.  Professional assistance should be sought with respect to the specification and construction of a specific project:

Preparation of Base for Pavers:  Remove excess soils and unstable subbase materials.  Compact subgrade to 95% proctor density test.

Paver Base Installation:  Backfill excavated area with appropriate depth aggregate material as specified in Unit Paver Section.  Base shall be compacted in 2 to 3 lifts to achieve proper density.  The base needs to extend 6 inches (152 mm) to 12 inches (305 mm) beyond the edge of paver installation.  Screed sand (or equivalent material as specified) over base to uniform thickness of not less than 1 inch (25 mm) and not more than 1-1/4 inches (32 mm).

After installation of restraint edging and pavers:  Sweep fine sand (or equivalent material as specified) into joints.  Make several passes with a plate compactor with no less than 3,000 - 5,000 lbs. (1,361 kg - 2,268 kg) centrifugal compaction force and operates at 80 to 90 hertz.  Continue sweeping sand into joints.  Make several passes alternating direction of compactor each time.  Remove excess sand from paver installation.

  - INSTALLATION OF PAVER RESTRAINT EDGING

Actual article number will be determined by location within the Part 3 portion of specification.

    - Preparation:  Ensure that all underground utility lines are located and will not interfere with the proposed edging installation before beginning work.

    - Locate border line of edging with string or other means to assure border straightness and curves as designed.

    - Edging Installation:  Install base of edging resting on compacted level base and facing [away from] [towards and under] paver, drive 3/8" x 10" (9.5 mm x 242 mm) bright spiral steel spikes through edging holes in section base of paver restraint edging at spaces for following applications:

      - Anchor each section end with spike.

      - Patios and Walkways:  12 inches (305 mm) to 24 inches (610 mm) on center.

    - Securely connect sections together in accordance with manufacturer’s instructions.

    - Install pavers.

May 1, 2003