ProSlide:  SHORT SPECIFICATION

Place the following in specification section that will be used for the main landscaping work (for example, Section 02900 Landscaping, or Section 02930 Exterior Plants, or etc.).  The architect to edit size, thickness, length, and finish required for the project.  Comments shown in “italics.”

- GENERAL

  - WARRANTY

Actual article number will be determined by location within the Part 1 portion of specification.

    - 15-year limited material warranty for landscape edging from manufacturing defects in workmanship or material.

- PRODUCTS

  - PLANTING ACCESSORIES

Actual article number will be determined by location within the Part 2 portion of specification.

    - Heavy Duty Straight Profile Edging:  Permaloc ProSlide, 1/8 inch (3.2 mm) x 4" (102 mm) [5-1/2" (140 mm)] high, 3/16 inch (4.8 mm) x 4" (102 mm) [5-1/2" (140 mm)] high, extruded aluminum, 6063 alloy, T-6 hardness, landscape edging for straight-line and curvilinear applications in corrugated straight profile, as manufactured by Permaloc Corporation, Holland MI 49424, telephone (800) 356-9660.  Section shall have loops on side of section to receive stakes spaced approximately 3 feet (915 mm) apart along its length.

    - Thickness:  1/8 inch (3.2 mm) gage section at 0.055 inch (1.40 mm) minimum thick with 0.26 inch (6.6 mm) exposed top lip and 3/16 inch (4.8 mm) gage section at 0.099 inch (2.51 mm) minimum thick with 0.298 inch (7.57 mm) exposed top lip.

    - Length:  16 feet (4.88 meters), selected products in 8 feet (2.44 meters) sections.

    - Connection Method:  Section ends shall slide together with a telescoping stakeless design.

    - Stake:  12 inch (305 mm) extruded aluminum stake, 0.125 inch (3.2 mm).  Stakes to interlock into section loops.

    - Finish: Natural Mill Aluminum, Black DuraFlex Painted, Green DuraFlex Painted, Bronze DuraFlex Painted, and Black Anodized (Class II).  Paint finish shall comply with AAMA 2603 for electrostatically baked on paint.

- EXECUTION

  - LANDSCAPE EDGING INSTALLATION

Actual article number will be determined by location within the Part 3 portion of specification.

    - Preparation:  Ensure that all underground utility lines are located and will not interfere with the proposed edging installation before beginning work.  Locate border line of edging with string or other means to assure border straightness and curves as designed.  Dig trench 1 inch (25 mm) deeper than set of edging bottom.

    - Set edging into trench with top at ½ inch (12.7 mm) above compacted finish grade on turf side with side having loops for stakes placed on opposite side of turf.  Drive stakes through edging loops until locked in place.  Requires 5 stakes evenly spaced for each 16 feet (4.88 meters) section, or 3 stakes evenly spaced for each 8 feet (2.44 meters) section.

    - Connect adjacent edging sections by sliding the ends into each other with a minimum of 2 inches (50.8mm) of overlap.

    - Where edging sections turn at corners and at angled runs, cut edging partially up through its height from bottom and turn back to desired angle to form rounded exposed radius.

    - Backfilling and Cleanup:  Backfill both sides of edging, confirm and adjust if necessary that sections are securely held together, and compact backfill material along edging to provide top of edging at 1/2 inch (12.7 mm) above turf finish grade.  Cleanup and remove excess material from site.

January 1, 2010